PRODUCTION INFORMATION

3 PLY DISPOSABLE FACE MASK



FEATURES

NON STERILIZED DISPOSIBLE MASK WITH EAR LOOPS

LATEX FREE

MATERIALS

OUT LAYER 20gsm polypropylene

FILTER LAYER MELBLOWN 21gsm polypropylene


INNER LAYER 25gsm polypropylene

EARLOOPS polyamide + polyurethane

NOSE BAR flexible plastic laminated with aluminum wire

WEIGHT 2.7gr.

GRAPH



Diamension:

A=17.5cm +/- 0.5cm

B=9.5cm +/-0.5cm

Length of latex free elastic: 16.5cm

Nose bar length: 10.8cm

Biocompatibility: non cytotoxi, non irritant and non sensitive

Bacterial Filtration Effeciency: 99%

Mean particle size(MPS): 3um

Breathing resistance: Delta P<49 Pa/sqcm